**BLS A3 3193**

**PVC COMPOUND FOR CABLE SKIN INSULATION**

**DESCRIPTION**

BLS Polymers Ltd. introduces compound for insulation of Cables – **BLS A3 3193** Compoundfor skin insulation of cables with maximum operating temperature of 70⁰C and minimum -15⁰C. This compound meets the stringent quality requirements for manufacturing of skin (thin) insulation for various types of wires and cables at high line speeds and provides protection against moisture and abrasion.

**STANDARD COMPLYING**

**BLS A3 3193** Compoundmeets the requirements of raw material for manufacturing of Type A Insulation as per ASTM, EN 50525-2-31, BS7655 Sec 3.1(TI1), IEC 60502-1(Type A) and IS 694 and IS 5831.

**SPECIAL FEATURES**

**BLS A3 3193** Compound provide very effective features as:

* Good mechanical properties
* High line speed
* Easy processability
* Easy color-ability

**TECHNICAL CHARACTERISTICS**

|  |  |  |  |
| --- | --- | --- | --- |
| **PROPERTY** | **TEST METHOD** | **UNIT** | **TYPICAL VALUE** |
| Density | ASTM D 792 | gm/cc | 1.31±0.02 |
| Tensile Strength at Break | IS 10810-P7, IEC 60811-1-1 | MPa | ≥19 |
| Elongation at Break | IS 10810-P7, IEC 60811-1-1 | % | ≥350 |
| Mechanical properties after ageing at 80±2⁰C for 7 days | | | |
| Variation of Tensile Strength at Break | IS 10810-P11, IEC 60811-1-2 | % | ±20 |
| Variation of Elongation at Break | IS 10810-P11, IEC 60811-1-2 | % | ±20 |
| Loss of Mass at 80±2°C for 7 days | IS 10810-P10, IEC 60811-3-2 | Mg/cm2 | ≤ 2.0 |
| Thermal stability 200°C±0.5°C | IS 10810-P60, IEC 60811-3-2 | Minute | ≥ 110 |
| Hardness | ASTM D 2240 | Shore A | 93±2 |
| Volume Resistivity at 23ºC | ASTM D 257 | ohm-cm | > 1 X 10^14 |
| Limited Oxygen Index | ASTM D 2863 | % | >26 |

\*Tests have been carried out on extruded sample/pressed sheet from granules of **BLS A3 3193**.

It is also available in Black and Colored, UV Stabilized variant. Preliminary tests are recommended in case of critical applications.

**PROCESSING GUIDELINES**

**BLS A3 3193** Compound can be processed in a normal PVC extruder with L/D ratio 24:1. Preheating of Granules at 70ºC for 2 hours is recommended. Suggested temperature profile for processing:

Extruder Zones Temperature profile

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Zone 1 | Zone 2 | Zone 3 | Zone 4 | Head | Neck & Die |
| 140±5ºC | 150±5ºC | 160±5ºC | 165±5ºC | 170±5ºC | 170±5ºC |

**STORAGE**

**BLS A3 3193** Compound must be stored in ambient temperature (not exceeding 35ºC) in a shaded area in sealed and intact bags to avoid exposure to sunlight and moisture. The shelf life of this compound is twelve months but long storing may affect the properties and processability of the compound and for this reason it should be used within 6 months from the manufacturing date. It is better to preheat the material before use.

**PACKING**

**BLS A3 3193** Compound is available in 25 kg bags with liners and 1000 kg Bulk bags. Other packaging is available on request.

We offer our Technical Services for further information and suggestion in using the product from the beginning and also for any need during the course of the product being used.

**Disclaimer:**

The products mentioned herein are not intended for use in medical, pharmaceutical or healthcare applications and we do not support their use for such applications. To the best of our knowledge the information provided herein is accurate and reliable as on date, and is provided in good faith as reference point with respect to the product described here. BLS Polymers makes no warranties which extend beyond the description contained herein. There is no guarantee and/or warrantee what so ever, after processing. In any case, BLS liability shall be restricted to the replacement of material in packed condition. It is the customer's responsibility to inspect and test our products in order to satisfy itself as to the suitability of the products for the customer's particular purpose. The customer is responsible for the appropriate, safe and legal use, processing and handling of our products. No liability can be accepted in respect of the use of BLS Polymers products in conjunction with other materials. The information contained herein relates exclusively to our products when not used in conjunction with any third-party materials. This information is intended to be used only as guideline for designers and processors of thermoplastics for extrusion. Because extrusion is complex, a set solution will not solve all problems. Observations on a trial-and-error basis may be required to achieve desired results. Data are obtained from specimens molded under carefully controlled conditions from representative samples of the product described herein. Properties may be materially affected by extrusion techniques applied and by the size and thickness of the item extruded. No assurance can be implied that all extrusion articles will have the same properties as those listed.